# Info Nr. 37.1

Behaviour of AF/Armaflex, Armaflex AC and SH/Armaflex against liquids, vapours, gases and solid substances, (in accordance to DIN 53 428 "check of foam materials")*

legend: 	      	+    	= 	unchanged

1    	= 	traces of attack

- = 	slightly attacked

- =	moderately attacked

4     	= 	strongly attacked

5	=	very strongly attacked

| substance | concentration |  | testing period |
| --- | --- | --- | --- |
|  |  | 1 h | 24h | 7d | 14d | 28d |
| 1.2 Dichlorethane | 99% | 3 | 3 | 4 | 5 | 5 |
| Acetone | 100% | 2 | 3 | 4 | 5 | 5 |
| Acetic Acid | 20% | + | 1 | 2 | 2 | 2 |
| Ammonia | gaseous (1,17*10-2%) | + | + | + | + | + |
| Ammonia, in water solution | 32% | 1 | 3 | 5 | 5 | 5 |
| Ammonium phosphate | 30% | 1 | 1 | 1 | 2 | 2 |
| Ammonium sulphate | 30% | 1 | 1 | 1 | 2 | 2 |
| ASTM Oil No. 1 (PAE 15960) | 100% | 1 | 2 | 2 | 2 | 2 |
| ASTM Oil No. 2 (PAE 15961) | 100% | 1 | 2 | 3 | 3 | 3 |
| ASTM Oil No. 3 (PAE 15962) | 100% | 1 | 3 | 3 | 3 | 4 |
| ASTM Oil No. 5 (PAE 15768) | 100% | 1 | 2 | 2 | 3 | 3 |
| Benzil alcohol | 99% | 2 | 3 | 3 | 4 | 5 |
| Butyl acetate | 98% | 2 | 2 | 4 | 5 | 5 |
| Chloroform | 100% | 2 | 3 | 4 | 5 | 5 |
| cleaner Desmofix K | 10% | + | + | 2 | 2 | 2 |
| Desinfection substance Pursept-AF | 1% | + | 1 | 2 | 2 | 2 |
| Dichlormethane (Methyl Chloride) | 100% | 2 | 4 | 5 | 5 | 5 |
| Ethylene acetate | 100% | 2 | 3 | 3 | 4 | 5 |
| Ethyl-methyl-keton | 99% | 2 | 2 | 4 | 5 | 5 |
| Hexan | 100% | + | 1 | 1 | 2 | 2 |
| Hydrogene peroxide | 3% | + | + | 3 | 3 | 3 |
| Isobutyl acetate | 100% | 1 | 2 | 3 | 5 | 5 |
| Nitric acid | 20% | + | 1 | 3 | 3 | 4 |
| Paraffin | 100% | + | 2 | 2 | 2 | 2 |
| Propan-2-ol (Isopropyl alcohol) | 100% | + | + | 1 | 2 | 2 |
| See water | 2,8% NaCl, 0,7% MgSO4, 0,5% MgCl2, 0,24% CaCl2, 0,2% NaHCO3 | 1 | 1 | 2 | 2 | 2 |
| Sodium carbonate (soda) | saturated solution | 1 | 1 | 1 | 2 | 2 |
| Sodium chloride (common salt) | saturated solution | 1 | 1 | 2 | 2 | 2 |
| Sodium hydroxide (caustic soda) | 40% | + | 1 | 1 | 1 | 1 |
| Sodium sulphate (Glauber salt) | saturated solution | 1 | 1 | 1 | 2 | 2 |
| Sulphuric acid | 20% | 1 | 2 | 2 | 2 | 2 |
| Xylene (Dimethylbenzene) | 97% | 1 | 2 | 4 | 5 | 5 |

All statements and technical information are based on results obtained under typical conditions. It is responsibility of the recipient to verify with us that the information is appropriate for the specific use intended by the recipient.